BIO-DUR®

560

FOR APPLICATION

ABOVE OR BELOW

WATER

###### PRODUCT DATA SHEET

BIO-DUR® 560 is based on a unique blend of liquid epoxy polymer and aliphatic polyamine curing agents, which is able to displace water from wet surfaces in order to make a permanent bond. The formulation is solvent-free to ensure safety and maximum technical performance. Kevlar* fibers are incorporated for reinforcement and viscosity management to achieve high application rates -even underwater!

BIO-DUR® 560 provides permanent protection under the most adverse conditions. The formula is uniquely field-friendly and uses advanced low toxicity ingredients in a high build brushable/rollable product. The sister product BIO-DUR® 561 is available if a higher viscosity; "light paste" consistency is required.

BIO-DUR® 560 can be shipped by Ground "Non-Regulated" by USDOT.  When shipped by Air or Ocean BIO-DUR® 560 is classified UN3082, PGIII.

* Kevlar is a trademark of E. I. Dupont de Nemours Co.

ANTICORROSIVE COATING: Splash zone, excellent abrasion resistance above or below water.

REPAIR COMPOUND: Patching, leak sealing etc. above and below water.

FIELD JOINT COMPOUND: Rapid curing, surface tolerant and excellent cathodic disbondment properties.

ENCAPSULATING COATING: Smooth, dense, easily decontaminated coating for steel and concrete. WASTEWATER: Reinforces, smooths and protects concrete exposed to chemical or municipal waste.

VEHICLE TYPE …………………………	Epoxy/Aliphatic amines

PIGMENTATION …………………………	Color/Inert/fibrous reinforcement

COLORS …………………………………	Standard White, Black, Gray – other available

FINISH ……………………………………	Slight texture

THINNER ………………………………...	Not normally required

CLEANER ………………………………... 	MEK or lacquer thinner

MIXING RATIO …………………………	1.0/1.0 v/v

INDUCTION TIME . ………………………	Not required

POT LIFE  …………………………………	Approx. 40’/ 77F

FLASH POINT …………………………… Over 200F

SOLIDS BY VOLUME ……………………	100%

SPREADING RATE/GAL…………………	1604 mil/sq.ft./gal, 53.5 sq.ft./gal @ 30 mils

DRY TIME, (Dust free) …………………….4 hours at 77F

DRY TIME, (Service)………………………	 24 hrs. heavy service at 77’F

APPLICATION METHOD……………….. 	Brush, roller, heated plural airless spray

STORAGE CONDITIONS…………………	Normal, Freezing OK

VOC. ……………………………………….	Essentially zero

DENSITY…………………………………...Base 9.6 lb/gal; Cure 13.0 lb/gal, Mix 11.3 lb/gal

SURFACE PREPARATION: Remove marine biological settlement and corrosion by >5,000 psi water jetting with or without abrasive. Conventional air/abrasive blasting works well at shallow depths however efficiency falls off sharply below, say, 10'. Hand held power tools such as needle guns or grinders can give good results if applied conscientiously in small areas but will be inadequate in large areas. Plan to apply the BIO-DUR®560 within 45 minutes maximum after surface preparation to minimize rerusting or initial settlement of fouling slime, which interferes with initial adhesion.

Application above water requires similar high pressure water blasting or dry abrasive blasting to yield a firm, granular surface free of loose contamination.

MIXING PROCEDURE: BIO-DUR® 560 is supplied in 2 gallon kits of 2xl containers each of epoxy base and curing agent. These components are formulated in contrasting colors to facilitate complete mixing.  Visible streaks of either component seen during the course of mixing indicate "hotspots" of unmixed components. It is imperative to properly mix the components since unmixed "hotspots" of either base or curing agent will never cure.

Remove equal quantities of base and curing agent from their cans and place them in a clean plastic or steel container. Mixing is accomplished by stirring with a "Jiffy" type mixer in a geared down, (high torque), 1/2" electric drill. Once mixing begins, there will be about 20 minutes of working time available at 77F. This time may be extended by keeping the components and mixture cool, rather than leaving it in a hot area.

APPLICATION:

1) Using a stiff brush or roller apply mixed components from a tray aiming for a wet film thickness of 30 mils, 	coverage rate of about 50 sq.ft. per gallon.

2) Apply by heated plural component airless spray using the following equipment setup:

Spray Unit:	Graco "King" or similar with heated hoses.

Mix ratio: 	1/1 by volume

Fluid pressure: 	2,500 psi

Fluid temp: 	140F

Filters: 		Remove all filters

Tip size: 	.029" -.039" orifice

CURING BEFORE SERVICE: BIO-DUR® 560 may be immersed in fresh or salt water immediately after application. It will cure to a hard film within about 8 hours and is suitable for traffic after this time. Allow at least three (3) days at 77F before subjecting to aggressive chemical service from industrial solvents and similar materials.

TYPICAL PHYSICAL PROPERTIES OF THE CURED FILM:

Compressive strength:	7,380 psi (50.9 N/mm2)

Tensile Strength:	6,000 psi (est.)

Flexural Strength:	4,550 psi (31.4 M/mm2)

Abrasion Resistance:	34.0 mg/1,000 cycles (CS17 wheels with 1,000 gram weights)

Tensile Adhesion:	>2,000 psi (“Near White” SA2.5 abrasive blasted dry steel)

“           “		>1,000 psi (>5,000 psi water jetted steel applied/cured underwater)

“           “		>1,000 psi (Power tool cleaned then >2,500 psi water jetted dry steel)