GasPruf 132

REINFORCED EPOXY COATING FOR APPLICATION ON HYDROCARBON CONTAMINATED SURFACES

###### PRODUCT DATA SHEET

GasPruf 132 is a unique blend of liquid polymers and proprietary curing agents which is able to displace water or hydrocarbons such as gasoline or diesel fuel from contaminated surfaces in order to make a permanent bond. The formulation is solvent-free to ensure safety and maximum technical performance. Kevlar fibers are incorporated for reinforcement and viscosity management to achieve high application rates -even under water or hydrocarbon liquids!

GasPruf 132 is designed for use on pipelines and similar surfaces where high performance epoxy materials must be applied on surfaces wetted with water and/or hydrocarbon fuels.  Consult TFT to discuss suitability for use in the presence of other organic liquids.

The standard color is brown however other colors are available in quantity and can be shipped by Ground "Non-Regulated" by USDOT.  When shipped by Air or Ocean GasPruf 132 is classified UN3082, PGIII.

* Kevlar is a trademark of E. I. DuPont de Nemours Co

ANTICORROSIVE COATING: “Super-Duty” anticorrosive for in-service fuel storage tank interiors and roofs.

REPAIR COMPOUND: Patching, leak sealing etc. above and below water or hydrocarbon fuels.

VEHICLE TYPE …………………………	Proprietary liquid polymers with curing agent

PIGMENTATION …………………………	Color/Inert/fibrous reinforcement

COLORS …………………………………	Standard Brown

FINISH ……………………………………	Slight texture

THINNER ………………………………...	Not required

CLEANER ………………………………... 	MEK or lacquer thinner

MIXING RATIO …………………………	1.0/1.0 v/v

INDUCTION TIME . ………………………	Not required

POT LIFE  …………………………………	Approx. 10’ / 77F

FLASH POINT …………………………… Over 200F

SOLIDS BY VOLUME ……………………	100%

SPREADING RATE/GAL…………………	40 sq. ft./gal @ 40 mils rec. U/W application rate.

DRY TIME, (Dust free) …………………….1 hour at 77F (in air)

DRY TIME, (Service)………………………	8 hrs. light, 24 hrs. heavy

APPLICATION METHOD……………….. 	Trowel, “Pool float”, mitts

STORAGE CONDITIONS…………………	Between 35’F – 95’F in original sealed containers

VOC. ……………………………………….	Essentially zero

SURFACE PREPARATION: Remove loose corrosion products using suitable abrasive techniques to leave a coarse, sound surface.  Suitable preparation techniques would include needle-scaling with sharp needles or abrasive discing.

Application above water requires similar preparation and would include high pressure water blasting or dry abrasive blasting to yield a firm, granular surface free of loose contamination.

MIXING PROCEDURE: GasPruf 132 is supplied either in 2 gallon or 4 gallon kits of 2x1 or 2x2 gallon containers respectively each of polymer base and curing agent. These components are formulated in contrasting colors of Red base and Green curing agent to yield a dark brown color on mixing.  Visible streaks of either Red or Green seen during the course of mixing indicate "hotspots" unmixed components which will never cure.

For small repairs remove equal quantities of base and curing agent from their cans and place them side-by-side on a surface of plastic, fiberboard etc. Mixing is easily accomplished by folding the components into each other using a spatula such as a tongue depressor or paint mixing stick. Once mixing begins there will be about 10 minutes of working time available at 80F. This time may be extended by keeping the components and mixture cool, avoid leaving mixed material on a hot deck.  Storing the unmixed components in an air-conditioned space prior to using will ensure that the mixture starts out cool in order to further extend its useful life.

APPLICATION:

1) ABOVE WATER: Apply using an appropriate tool such as a spreader or short, stiff brush if the surface is especially rough.

2) UNDER GASOLINE OR DIESEL FUEL:  If the surface is safely accessible to personnel simply apply by spreader or brush.

CURING BEFORE SERVICE: GasPruf 132 may be immersed in gasoline, diesel fuel, fresh or salt water immediately after application. It will cure to a hard film within about 4 hours and is suitable for traffic after this time. Allow at least a day at 77F before subjecting to aggressive service from industrial solvents and similar materials.