Thin Film Technology, Inc.

TECHNICAL INFORMATION

RECOMMENDED USES

PRODUCT DATA SHEET

BIO-SEAL™ 192 is based on pure liquid epoxy polymers and proprietary polyamine curing agents.

BIO-SEAL™ 192 is formulated with no volatile solvents and is so completely tolerant of water that it may be applied to damp or wet surfaces yet still function well as a reinforcing seal coating. Applications may be made using brush or roller with no especial ventilation requirements -odor during application is almost completely absent.

BIO-SEAL™ 192 is an ideal saturating resin for use with fiberglass, basalt or carbon fibers, its field-friendliness and lack of odor ensure the best possible worksite conditions.

BIO-SEAL™ 192 can be shipped by Ground "Non-Regulated" by USDOT.  When shipped by Air or Ocean BIO-SEAL™ 192 epoxy base is classified UN3082, PGIII only when packed in containers larger than 5L/1.33 gallons.

BIO-SEAL™

192

EPOXY RESIN FOR EPOXY MORTAR AND COMPOSITE REPAIR

BIO-SEAL 192 is designed for ease of use in the field.  It has excellent adhesion to metals such as stainless and carbon steel.  When fully cured the resin has a wide resistance to industrial commodities such as gasoline, diesel fuel, crude oil and other hydrocarbons.  These characteristics make it ideal for industrial applications such as pump base primer.

EPOXY MORTAR REPAIRS:  BIO-SEAL 192 is an effective epoxy resin for use making rapid setting mortar for industrial applications such as pump bases where high strength with rapid set is required.

COMPOSITION: Vehicle Type…….…………………..	Epoxy/Polyamines

Pigmentation………….………………	None

Solids by Volume…………………….	100%

Flash Point …………………………..	Over 212F

VOC	…………………………………	Essentially Zero at normal ambient temperatures

APPEARANCE:  Gloss ………………………………...	Matte when fully absorbed, unabsorbed is full gloss

Color…………………………………	Clear, slightly amber

APPLICATION:  Methods ……………………………...	Brush, roller

Rec. Dry Film Thickness. …………..	N/A

Rec. Wet Film Thickness…………….	N/A

Coverage, (theor.). …………………..	N/A

Induction Time ………………………	Not Required – may be used immediately after mixing

Pot Life……………………………….	Approx. 35’ @ 77F, (25C)

Dry Time – Dust Free ………………..	4 hours @ 77F, (25C)

Dry Time - Service…………………..	12 -24 hours light service @ 77F, (25C).  Fully cured in 3 days at 77’F

STORAGE:	   Shelf Life……………………………..	24 months under normal storage conditions

TRANSPORTATION…………………………………	USDOT, IATA, & IMO “Non-Regulated” when         shipped in 2 gallon or smaller kit sizes.

SURFACE PREPARATION:

Bare Concrete: surfaces should be allowed to cure for a minimum of 20 days before coating. Excessive weak

surface laitance must be removed by either acid etching or, preferably, abrasive sweeping before coating. Aged, uncoated concrete surfaces are best prepared by abrasive sweeping. Unless carried out properly acid etching can give unpredictable results due to inadequate etching or inadequate rinsing, for this reason abrasive blasting is the preferred method of preparation. Contamination by oil or grease should be removed, with an industrial degreaser before either abrasive blasting or acid etching.

Steel surfaces:  BIO-SEAL™ 192 is most commonly used with reinforcing fiber on steel surfaces for reinforcing and sealing purposes.  When used with carbon fiber it is recommended to apply an initial cathodic sealing coat of either BIO-DUR 290 epoxy coating or a first layer of non-conductive fiberglass or basalt composite to insulate the underlying steel from possible cathodic effects.  Prepare the steel by abrasive blasting to SSPC-SP-10, “Near-White” standard with a 2 – 4 mil anchor profile for best results.  Small areas may be prepared using mechanical tools such as needle scalers or abrasive disks.

MIXING PROCEDURE: BIO-SEAL™ 192 is supplied in 2 gallon kits of comprising epoxy base in a part filled 2 gallon plastic pail with curing agent packed in a part filled one gallon steel can. A "Jiffy" type mixer with a high torque motor is recommended for proper blending. Pour the curing agent into the base and mix for about 2 minutes taking care to stir in all base material from the edges and base of the plastic pail, unmixed material will never harden. No induction or "sweat-in" time is required and the mixed material may be used immediately.

When using with sand or other inert mineral aggregate as a mortar first thoroughly mix a two-gallon BIO-SEAL™

192 kit using a 1/2" "Jiffy" type mixer then pour this mixed material into a larger container such as a clean five gallon pail. Using the same Jiffy mixer add the desired mineral aggregate while stirring until the desired viscosity is obtained. As a guide it will be found that a two-gallon kit of BIO-SEAL™ 192 will accept about 66 lbs of sand to yield five gallons of a heavy but flowable mortar. This mortar can be used to smooth and level concrete, set safety railings into holes and so on. Addition of more sand will yield a stiffer mortar, which can be applied in heavy thickness without sagging. Fine sand makes a stiffer mortar than coarse sand. Sharp sand makes a stiffer mortar than rounded sand.

Pot life and reaction time is heavily dependent on temperature, as a general guide figure that each 18F, (10C), variation in temperature above or below 77F, (25C), will respectively halve or double the pot life and cure times.

APPLICATION: Brush or roller application is straightforward and requires no special technique.

CURING AND TEMPERATURE RANGE IN SERVICE: At 25°C/77°F BIO-SEAL™ 192 will cure to a hard film within 8 hours and is suitable for handling and light service after this time. Allow at least three (3) days at 77F before subjecting to aggressive chemical service from industrial solvents and similar materials.  After full curing BIO-SEAL 192 can operate in the temperature range of -40°C/F to 180°F/82°C in wet service and -40°C/F to 275°F/135°C.

TYPICAL PROPERTIES OF CURED BIO-SEAL 192:

Compressive Strength:			10,000+psi

Tensile Strength:			  7,000+ psi

Tensile Elongation, (Flexibility):	3.2%

Hardness (Shore D):			78

Glass Transition Temp:			122’F