BIO-SEAL™

193

CHEMICAL RESISTANT

HIGH TEMPERATURE EPOXY LAMINATING RESIN

PRODUCT DATA SHEET

BIO-SEAL™ 193 is based on pure, chemical resistant liquid epoxy polymers and proprietary polyamine curing agents.  It is formulated with no volatile solvents. Applications may be made using brush or roller with no especial ventilation requirements -odor during application is almost completely absent.

BIO-SEAL™ 193 is especially chemical resistant to almost all industrial commodities including caustics, hydrocarbon and most oxygenated solvents and acids such as concentrated sulfuric. BIO-SEAL 193 cures fully at normal ambient temperatures yet is heat resistant to at least 400°F/204°C.

BIO-SEAL™ 193 can be shipped by Ground "Non-Regulated" by USDOT.  When shipped by Air or Ocean BIO-SEAL™ 193 is classified UN3082, PGIII except when the base is shipped in <5L, (<1.32 gallons), when it is classified as NonHazmat per SP A197.

PENETRATING SEALER -used to seal and protect concrete, brick and similar surfaces against chemical attack, and penetration by water leading to chloride and freeze-thaw damage.

COMPOSITE RESIN:  works well with fiberglass, basalt and carbon fabrics to create heat resistant field-applied composites.

COMPOSITION: Vehicle Type…….…………………..	Epoxy/Polyamines

Pigmentation………….………………	Unpigmented

Solids by Volume…………………….	100%

Flash Point ……………………………Over 212F

VOC ………………………………….	Essentially Zero

APPEARANCE:  Gloss ………………………………...	Matte when fully absorbed, unabsorbed is full gloss

Color…………………………………	Clear

APPLICATION:  Methods ……………………………...	Brush, roller or spray

Rec. Dry Film Thickness. …………...As specified

Rec. Wet Film Thickness…………….As specified

Coverage, (theor.). …………………..	100 sq.ft./gallon @ 16 mils thickness

Induction Time ………………………	Not Required - may be used immediately after mixing

Pot Life……………………………….	Approx. 35’ @ 77F, (25C)

Dry Time – Dust Free ………………..8 hours @ 77F, (25C)

Dry Time - Service…………………..	24 hours handling, 36 hours light service @77F, (25C)

STORAGE:	   Shelf Life……………………………..	12 months under normal storage conditions

TRANSPORTATION: ……………………………….…“Non-Regulated” for ground transportation.  UN3082, PG

III, “Environmentally Hazardous Substance, Liquid N.O.S.”

SURFACE PREPARATION:

Bare Concrete: surfaces should be allowed to cure for a minimum of 20 days before coating. Excessive weak surface laitance must be removed by either acid etching or, preferably, abrasive sweeping before coating. Aged, uncoated concrete surfaces are best prepared by abrasive sweeping. Unless carried out properly acid etching can give unpredictable results due to inadequate etching or inadequate rinsing, for this reason abrasive blasting is the preferred method of preparation. Contamination by oil or grease should be removed with an industrial degreaser before either abrasive blasting or acid etching.

High pressure water-jetting using minimum 3,500 psi held close-in is ideal for architectural concrete surfaces.  Allow to dry before application of BIO-SEAL 193 in order to permit absorption into the concrete surface.

MIXING PROCEDURE: BIO-SEAL™ 193 is supplied in 2 gallon kits of comprising epoxy base in a part filled 2 gallon plastic pail with curing agent packed in a part filled one gallon steel can. A "Jiffy" type mixer with a high torque motor is recommended for proper blending. Pour the curing agent into the base and mix for about 2 minutes taking care to stir in all base material from the edges and base of the plastic pail, unmixed material will never harden. No induction or "sweat-in" time is required and the mixed material may be used immediately.

Pot life and reaction time is heavily dependent on temperature, as a general guide figure that each 18F, (10C), variation in temperature above or below 77F, (25C), will respectively halve or double the pot life and cure times.

APPLICATION: Brush or roller application is straightforward and requires no special technique. Application on a floor is assisted by using a squeegee to distribute the BIO-SEAL™ 193 then backrolling to achieve an even coating. The material will thicken in cold weather and will be noticeably heavier at temperatures of 50'F and below.

When used as a resin for composite creation it is recommended to work on a horizontal surface covered with heavy duty polyethylene.  Before placing the fiber on this surface prime with a first coat of BIO-SEAL 193 in order to begin the saturation of the underside.  Pour mixed material onto the top surface and spread with a straight-edge, roller or brush as appropriate.  As saturation progresses fiberglass will be seen to become almost transparent.  After saturation roll up the wetted fabric onto a PVC pipe core in order to make application to surfaces such as piping easier.

When a glossy surface is desired over an absorbent substrate such as concrete or brick it will be necessary to apply at least two coats of BIO-SEAL™ 193. The first coat will penetrate and seal. After this seal coat has cured for about six hours minimum a "glaze coat" of BIO-SEAL™ 193 may be applied at about 5 mils thickness, (320 sq.ft. per gallon), to yield a tough, high gloss finish. A light broadcast of abrasive such as Aluminum Oxide or silica sand backrolled into this coat will provide enhanced slip resistance.

CURING BEFORE SERVICE: BIO-SEAL™ 193 will cure to a hard film within 24 hours and is suitable for traffic after this time. Allow at least three (3) days at 77F before subjecting to aggressive chemical service from industrial solvents and similar materials.