###### BIO-SEAL™

206

SOLVENT-FREE, HIGH TEMPERATURE EPOXY RESIN FOR COMPOSITES OR CRACK SEALING

PRODUCT DATA SHEET

BIO-SEAL 206 is a formulated using a combination of liquid epoxy resin and a special high temperature curing agent.  A unique feature of this combination is that although it has a high heat distortion temperature it still cures to a hard and “dust-free” condition at normal temperatures.  This feature is very useful since it permits convenient handling of laminates prior to final heat curing.

BIO-SEAL 206 has been tested as an external repair composite on a 30” pipe at 356°F, (180°C), at an operating pressure of 300 psi for over four months without failure.  Dry testing on steel indicates a temperature resistance up to about 500°F, (260°C).

Although the resin hardens at normal ambient temperature it must be heated to a minimum of 150°F/66°C for at least 3 hours for full curing.   Maximum Tg, glass transition temperature, is reached after heating to 302°F, (150°C).

BIO-SEAL 206 Epoxy base ships “Unregulated by Ground and as UN3082, PGIII by Air or Ocean unless packed in approved containers with <5L, (<1.32 gallon), contents.  The curing agent ships as UN2289, PGIII by Ground, Air or Ocean.

Saturating Resin for high temperature crack filling and composite production.

VEHICLE TYPE …………………………	Polyamine cured epoxy resin.

PIGMENTATION …………………………	None, (clear resin), or standard green

COLORS …………………………………	Amber colored or dark green after curing

FINISH ……………………………………	Full Gloss

THINNER ………………………………...	Not normally required

CLEANER ………………………………... 	MEK or lacquer thinner

MIXING RATIO …………………………	3.77/1.00 by weight, 3.14/1.00 by volume

INDUCTION TIME. ………………………	Not Required

POT LIFE …………………………………	Approx. 1 hr. / 77F, (100 gram mass).

FLASH POINT …………………………… Over 223°F/110°C (Unmixed Components)

SOLIDS BY VOLUME ……………………	100%

REQ. DRY FILM THICKNESS……………NA

SPREADING RATE/GAL…………………	231 cubic inches/gallon

DRY TIME, (Dust free) ……………………6 hours at 77F

DRY TIME, (To Handle)……………..…… Overnight at 77’F

APPLICATION METHOD……………….. 	Brush, Roller, Injection

STORAGE CONDITIONS…………………	Normal

VOC. ……………………………………….	Essentially zero

SURFACE PREPARATION:

Surfaces under composites should be free of dust, dirt, oils and moisture.  BIO-SEAL 206 can be applied over properly prepared steel, galvanizing, aluminum and concrete.

MIXING PROCEDURE:

BIO-SEAL 206 is supplied in kits of premeasured base and curing agent.  Use a suitable mixer to initially stir the base then pour in the curing agent and continue mixing for about one extra minute taking care to incorporate all material from the base and sides of the pail.  When supplied as green the epoxy base is dark blue and the cure is bright yellow, when thoroughly mixed these yield an attractive green with no stripes of unmixed components remaining visible.

APPLICATION:

Injection: Prepare cracks for filling using the normal ports and crack sealer.  Inject through lower ports into cracks until excess material is ejected from a higher level.  Seal ports as injection proceeds and ensure that the mass of concrete is heated to at least 150°F for at least 3 hours prior to service.

Composites:  Apply to the composite fabric using a brush or straight-edged spreader.  Place the fabric on a horizontal surface covered with plastic sheet – it is helpful to initially prime the plastic sheet with BIO-SEAL 206 in order to assist with saturation and to anchor the fabric to the surface.  Once impregnated roll up the fabric and unwind onto the surface being reinforced, usually piping, taking care not to create bubbles or blisters.  It is helpful to wrap the fresh resin and fabric with plastic “stricture” wrap in order to prevent draining of the resin and to create as dense a composite as possible.

Allow to cure until hardened then remove the stricture wrap and elevate temperature to at least 150°F for a minimum of three hours to properly cure the resin.  In order to achieve a glass transition temperature of 147°C/297°F a further two hours of heating to 150°C/302°F is required.  Note: although tack-free after initial hardening the 206 resin is still thermoplastic – it may deform during initial post-curing unless supported. A conservative maximum service temperature of is 356°F, (180°C), is recommended.

SHIPPING DATA:

Proper Shipping Name:	Epoxy Base:  Environmentally Hazardous Material, Liquid, N.O.S. (BisphenolA-Epichlorohydrin Liquid Epoxy Resin)

Curing Agent: Isophoronediamine mixture

UN Nos:				Base:	UN 3082 (Note: ships “NonHazmat” when packed <5L containers)

Cure:     UN 2289

Hazard Class:				Part A: Hazard Class 9, PGIII unless packed <5L, (<1.32 gal), containers.

Part B: Hazard Class 8, Corrosive, PGIII

Flash Point SETA:			Part A: >300°F/149°C

Part B: >230°F/110°C