TOWER-GARD

568

REINFORCED EPOXY ANTICORROSION COATING FOR CONCRETE, STEEL AND GALVANIZING

###### PRODUCT DATA SHEET

TOWER-GARD 568 is based on a unique blend of liquid epoxy polymer, toughening resins and aliphatic polyamine curing agents and is able to displace water from wet surfaces in order to make a permanent bond. The formulation is solvent-free to ensure safety and maximum technical performance. Kevlar fibers are incorporated for reinforcement and viscosity management to achieve high application rates – UV absorbers are incorporated into the formulation to resist degradation by exposure to intense sunlight.

BIO-DUR® 568 provides permanent protection under the most adverse conditions. The formula is uniquely field-friendly and uses advanced low toxicity ingredients. Standard color is Haze Gray.

BIO-DUR® 568 can be shipped by Ground "Non-Regulated" by USDOT.  When shipped by Air or Ocean BIO-DUR® 568 is classified UN3082, PGIII.

* Kevlar is a trademark of E. I. DuPont de Nemours Co

ANTICORROSIVE COATING: For concrete, structural steel and galvanized surfaces in atmospheric service.  TOWER-GARD 568 is uniquely tolerant of compromised surfaces.  TOWER-GARD 568 can be applied over all types of tightly adherent existing coatings as well as to bare concrete, steel or galvanizing.   Its surface tolerance and flexibility also ensure good adhesion to a variety of substrates such as tight residues of old coatings on steel and concrete.

VEHICLE TYPE …………………………	Epoxy, Flexibilizers and Aliphatic amines

PIGMENTATION …………………………	Color/Inert/fibrous reinforcement

COLORS …………………………………	Standard Haze Gray – others available

FINISH ……………………………………	Slight texture by brush, smooth by spray

THINNER ………………………………...	Not normally required

CLEANER ………………………………... 	MEK or lacquer thinner

MIXING RATIO …………………………	1.0/1.0 v/v

INDUCTION TIME. ………………………	Not required

POT LIFE …………………………………	Approx. 40min. / 77F

FLASH POINT …………………………… Over 200F

SOLIDS BY VOLUME ……………………	100%

SPREADING RATE/GAL…………………	80 sq. ft./gal @ 20 mils

DRY TIME, (Dust free) …………………….4 hours at 77F

DRY TIME, (Service)………………………	14 hrs. light, 72 hrs. heavy

APPLICATION METHOD……………….. 	Brush, roller, painters mitt, plural airless spray.

STORAGE CONDITIONS…………………	Normal

VOC. ……………………………………….	Essentially zero

SURFACE PREPARATION:

Painted Surfaces: TOWER-GARD 568 can be applied over all types of existing coatings or coating residue provided they are in generally fair condition and tightly adherent.  Remove loose surface contamination and worn coatings by sanding, discing, abrasive blasting or water jetting prior to application.

Application above water requires similar high pressure water blasting or dry abrasive blasting to yield a firm, granular surface free of loose contamination.

MIXING PROCEDURE: BIO-DUR® 568 is supplied either in 2 gallon or 4 gallon kits of 2x1 or 2x2 gallon containers, including one each of epoxy base and curing agent. It is important to thoroughly mix equal volumes of the two components as “hotspots” of badly mixed components will cure poorly.

Mix in a clean container using either paint stirrers for small quantities or a “Jiffy” style mechanical paint stirrer for larger quantities.  “Hotspots” of unmixed material will be seen as streaks and will never cure.

APPLICATION:

- Above water by brush or roller:  Use natural or synthetic fibers, it is generally not worth the effort to clean these tools after use.

- By Heated Plural Component Airless Spray:  The setup described below will give satisfactory results on larger jobs:

Equipment:		Graco “King”, 1/1 ratio units or similar heavy-duty pumps

Hose Pack Length:	Up to 160 feet of at least 3/8” – recommend heated and insulated hose pack.

Filters:			Remove all filters – these will clog with Kevlar fibers very quickly

Fluid Temperature:	Recommend 125°F - 135°F

Fluid Pressure:		2,500 – 3,000 psi at the tip

Tip Size:		minimum 0.031 thou”

Cleaning Solvent:	MEK or standard epoxy thinner

CURING BEFORE SERVICE:  TOWER-GARD 568 may be immersed in fresh or salt water immediately after application. It will cure to a hard film within about 14 hours and is suitable for light traffic after this time.